## Slide 1
Anwar Cement Sheet Limited
Industrial Practice

## Slide 2
Ashiqur Rahman Khan ID-201736004
Masum Mushfiq Dolon ID-201736011
Nazmus Shakib ID-201736029
Lipa Akter ID-201736009
MD. Niamul Ahsan ID-201736015
Shariful Islam ShiShir ID-201736042
Group Members
Military Institute of Science and Technology

## Slide 3
About Anwar Cement Sheet

## Slide 4
History
Ivory Comb and Button Manufacturing Network
Since 1834
Since 2014
Cement Sheet Manufacturing
Anwar Group of Industries

## Slide 5
Products
Anwar Cement Sheet
Plane Cement Sheet
Tua
Cement Mold
Corrugated Cement Sheet

## Slide 6
Introduction
Combination of Cement and Reinforcing Fibers
Fig 1: Cement
Fig 2: Asbestos

## Slide 7
Why Use Cement Sheet?
Cement sheet | Properties | GI sheet
Thick | Thickness | Thin
Heavy | Weight | Comparatively Light
High | Corrosion Resistivity | Low
High | Fire Resistivity | Low
High | Acid Resistivity | Low
Low | Temperature | High
High | Load Bearing Capacity | Comparatively Low

## Slide 8
Raw Materials Preparations

## Slide 9
Raw Materials
Cement Sheet
Mineral Fiber-Chrysotile
(12.25%)
Pulp-Jeans
(1%)
Cement
(86.5%)
Glass Fiber-
E Glass Chop
(.25%)
Binding and Structure
Increase Strength
Increase Flexibility

## Slide 10
Slurry Mixing Tank
Fiber Weigh Hopper
Buffer Silo
Edge Runner Mill
Blender
Lump Crusher
Bag Shredder
Bag Hooker
Bag Cutter
(Long and Side)
Bag Pushing Device
Chrysotile
Bucket Conveyor
Screw Conveyor
Blower
Belt Conveyor
Vertical Lift
Dust Collector
Dust
Bags
Fiber
Fiber Preparation
BOD
Fiber Preparation

## Slide 11
Pulp Preparation
Jeans from Local Garments
Pulp Warehouse
Shredding of Jeans by Cutting Machine
Beater Tank
200 kg pulp
+
1000 liter water
SM Tank
Day Tank
Hydro Pulp Tank
1200 liter
water
Pulp Dozing Tank
Water
from Cone Tank

## Slide 12
Cement Preparation
Cone Tank
Beater Tank
Cement Weigh Hopper
Cement Silo
SM Tank
Screw Conveyor
Water

## Slide 13
Slurry Mixing Tank

## Slide 14
Water Distribution

## Slide 15
Cement Sheet Production

## Slide 16
Main Machine

## Slide 17
Main Machine

## Slide 18
Passing
the Green
Sheet
Conveyor-1
Conveyor-2
Conveyor-3
Long Cutting
&
Painting
Cross Cutting
&
Piling
Waste
Waste
Waste
Side Conveyor Section

## Slide 19
Side Conveyor Section
Waste
Waste
Dissolver
Water
From
Cone Tank
Storage
Dilution
tank

## Slide 20
Side Conveyor Section
Conveyor-3
Forming Table
Stack of
Green Sheet
& Template
Plane Green
Sheet
Corrugated
Green Sheet
Template
Transfer
Car
Transfer
Car
VC Box
Heating Chamber

## Slide 21
Depiling Section

## Slide 22
Quality Control

## Slide 23
QC Standards (Fiber)
Characteristics | Value | Standards
Moisture | (35 ± 2) % | ACSL SOP
Buoyancy | 1800 cc | ACSL SOP

## Slide 24
QC Standards (Pulp)
Characteristics | Value | Standards
Pulp opening | Full Open | ACSL SOP
Consistency | As per Furnish | ACSL SOP
SR - Value | 22° to 26° | ACSL SOP

## Slide 25
QC Standards (Green Sheet)
Characteristics | Value | Standards
Moisture | (35 ± 2) % | ACSL SOP
Density (Dry) | 1.35 ± 0.05 gm/cc | ACSL SOP

## Slide 26
QC Standards (Green Sheet)
(75 ± 1) mm
21 mm

## Slide 27
QC Standards (Green Sheet)
4 to 10 ft
1065 ± 5 mm
No. of Corrugation = 14

## Slide 28
QC Standards (LBC Test)
Chart: 
| Day 28 | Day 21 | Day 14 | Day 7 | Day 1
 | 350 | 335 | 320 | 280 | 250

## Slide 29
Recommendations

## Slide 30
Limitations
Limitations
Frequent Breakdown
Overproduction
No Visual Representation
Analogue Data Collection
Low Quality Fiber
Double Line Production

## Slide 31
Fiber Quality
Chrysotile
Grade 6 Fiber
Low Quality
Low Cost
Mixture of Fiber of Different Grades
Linear Programming
Parameters
Cost
Grade
Strength
Optimum Quality
& Cost
Limitation
Recommendation

## Slide 32
Analogue Data Collection
Limitation
Recommendation
Manual Data Collection
Digital Input
Automated Data Collection
Visual Representation
Slight Deviations in Process
CUSUM
EWMA

## Slide 33
Overproduction
Limitation
Recommendation
Absence of Proper Market Analysis
Proper Forecasting
4p’s of Marketing
4p’s
Product
Price
Place
Promotion

## Slide 34
Frequent Breakdown
Limitation
Recommendation
Breakdown of Whole System
Software Breakdown
Schedule Maintenance of Software
Hardware & Software Integration

## Slide 35
Additional Recommendation
Current Situation
Recommendation
White Marks of Calcium on Cement Sheet
Water Curing
Environment of Heating Chamber
120°C Temperature
6 to 7 Bar Pressure
Water Curing With No White Marks
Increased Strength

## Slide 36
Additional Recommendation
Addition of Jute Fiber
Addition of Cotton with Jeans
Trial and Error
DOE
For Reducing Cost
For Promoting Local Resource
For Implementing Green Production

## Slide 37
Thank You For Your Attention

## Slide 38
Any Questions?